## Slide 1
MAUD School
Structural Analysis of Nanomaterials
using Electron Diffraction
Philippe BOULLAY
Cristallographie et Sciences des Matériaux – CRISMAT UMR 6508 CNRS – Caen, France
Electron Powder Diffraction : Rietveld analyses using MAUD
Intensity extraction from images pp. 02-08
Sizes, shapes and textures pp. 09-15
Structure refinements pp. 16-19
P. Boullay, L. Lutterotti, D. chateigner and L. Sicard, Acta Cryst. A 70 (2014) 448-456
Fast Microstructure and Phase Analyses of Nanopowders using Combined Analysis of TEM scattering patterns

## Slide 2
Intensity extraction along the rings by segments using an ImageJ plugin
Structural Analysis of Nanomaterials
using Electron Diffraction


only dependent of the specification of your CCD camera► pixel to mm
pixel size

## Slide 3
Intensity extraction along the rings by segments using an ImageJ plugin
Structural Analysis of Nanomaterials
using Electron Diffraction

Transmission geometry for TEM scattering experiments with the nomenclature used in MAUD
3°
120 patterns
CAKING
chi=phi=0° / omega=90° / eta: 0° to 360°

## Slide 4
Intensity extraction along the rings by segments using an ImageJ plugin
5°
72 patterns
CAKING
chi=phi=0° / omega=90° / eta: 0° to 360°
estimation of the center position using a reference circle on the screen
Structural Analysis of Nanomaterials
using Electron Diffraction


## Slide 5
Pawley fitting without refining center or tilting
Centre defined graphically on the image
Rwp = 2.83 %
Pawley fitting refining center but not tilting
x-center error = -0.00717(5) mm
y-center error = -0.01278(5) mm
Rwp = 2.32 %
Corrections for center position and elliptical distortion ?
Pawley fitting refining centre and tilting
x-center error = -0.00755(4) mm
y-center error = -0.01093(4) mm
tilting error x (sin(error)) = -0.0048(3)
tilting error y (sin(error)) = 0.1211(3)
Rwp = 1.56 %
Structural Analysis of Nanomaterials
using Electron Diffraction

## Slide 6
Intensity extraction along the rings by segments using an ImageJ plugin
5°
72 patterns
CAKING
chi=phi=0° / omega=90° / eta: 0° to 360°
estimation of the center position using a reference circle on the screen
Structural Analysis of Nanomaterials
using Electron Diffraction

we have to calibrate the distance specimen/detector ► mm to 2q
?
not important here BUT

## Slide 7
Intensity extraction along the rings by segments using an ImageJ plugin
Structural Analysis of Nanomaterials
using Electron Diffraction
calibrate the distance specimen/detector using a « reference material »
▼
▼
▼
▼
► an assembly of nanoparticles with known SG and lattice parameters
► best if microstructural features (size, shape, ….) are known (from XRPD)
Camera length read on the TEM (mm) | Apparent spec/detc distance (mm)
600 | 109.9
800 | 145.3
1000 | 180.6
1200 | 229.4
1500 | 271.2
2000 | 375.1

## Slide 8
Intensity extraction along the rings by segments using an ImageJ plugin
3°
120 patterns
CAKING
chi=phi=0° / omega=90° / eta: 0° to 360°
estimation of the center position using a reference circle on the screen
2D plot
Structural Analysis of Nanomaterials
using Electron Diffraction

## Slide 9
2q (°) => Q (Å-1)
b(x): background => pic at 0° + polynomial function
peak location and intensities
1D XRPD-like pattern (360° summed intensity)
measured profile h(x) = f(x)  g(x) + b(x)
Structural Analysis of Nanomaterials
using Electron Diffraction
peak broadening vs. dhkl

## Slide 10
h(x) = f(x)  g(x) + b(x)
sample contribution
instrumental broadening
Extraction of f(x) can be obtained by a whole-pattern (Rietveld) analysis
Line broadening causes
instrumental broadening
finite size of the crystals (acts like a Fourier truncation: size broadening)
imperfection of the periodicity (due to dh variations inside crystals: microstrain effect)
generally: 0D, 1D, 2D, 3D defects
All quantities are average values over the probed volume
► electrons, x-rays, neutrons: complementary
► distributions: mean values depend on distributions’ shapes
Need to know g(x) the instrumental broadening !
L. Lutterotti and P. Scardi, J. of Appl. Crystallogr. 23, 246-252 (1990)
The instrumental Peak Shape Function is obtained by analysing nanoparticules of known sizes and shapes as obtained from X-ray analyses
Structural Analysis of Nanomaterials
using Electron Diffraction

## Slide 11
Mn3O4 hausmannite
Bruker D8 / Lynx Eye 1D
l=1.54056 Å (Cu Ka1)
SG: I 41/a m d
a=5.764(2)Å and c=9.448(4)Å
TOPCON 2B / CCD ORIUS
l=0.0251Å
a=5.7757(2)Å and c=9.4425(4)Å
53 Å
64 Å
pattern matching
structure
POPA
anisotropic
shape
g(x) ► f(x)
f(x) ► g(x)
background substracted
Structural Analysis of Nanomaterials
using Electron Diffraction
TEM : poor resolution ! ►not for particles larger than 20 nm
Cagliotti function
U=3.32 10-4
V=-2.5 10-2
W=3.2

## Slide 12
TOPCON 2B / CCD ORIUS
l=0.0251Å
a=5.7757(2)Å and c=9.4425(4)Å
53 Å
64 Å
POPA
anisotropic
shape
f(x) ► g(x)
Structural Analysis of Nanomaterials
using Electron Diffraction
Mn3O4 hausmannite

## Slide 13
20nm
5°
72 patterns
Microstructure of nanocrystalline materials: TiO2 rutile (1)
M. Reddy et al., ElectroChem. Com. 8 (2006) 1299-1303
FEI Tecnai / CCD USC1000 / l=0.0197Å
from phase search: TiO2 rutile P42/mnm a= 4.592Å a=2.957Å (COD database ID n°9001681)
Structural Analysis of Nanomaterials
using Electron Diffraction

## Slide 14
XRPD
EPD
average anisotropic crystallite size
structure
pattern matching
4-circles diffract. / INEL CPS
l= CuKa
Structural Analysis of Nanomaterials
using Electron Diffraction
POPA (up to R4)

## Slide 15
decreasing the selected area
0.5μm
data
fit
no texture
Q (Å-1)
6μm
data
fit
E-WIMV
Q (Å-1)
intensity variation along the rings
Structural Analysis of Nanomaterials
using Electron Diffraction
Can be modelled in MAUD using texture
analysis

## Slide 16
Structural Analysis of Nanomaterials
using Electron Diffraction
pattern matching
structure factors
kinematical approx.


► microstructural features can be obtained in the pattern-matching mode
► not convincing using structure factors from kinematical approximation …
► Electron crystallography: more complicated than XRD due to dynamical conditions
Take into account dynamical conditions ?

## Slide 17
Structural Analysis of Nanomaterials
using Electron Diffraction
► Electron crystallography: more complicated than XRD due to dynamical conditions
2-beams or Blackman correction
ratio between the dynamical and kinematical intensity of a hkl reflection
(*) electron atomic scattering factors from the tables of L.M. Peng et al., Acta Cryst. A52 (1996) 257.
J0 is the zero order Bessel function, Fhkl is the kinematical structure factor(*), H is the thickness in Angstrom of the crystallite, Vc the cell volume, m and e are respectively the mass and charge of the electron, h the Planck constant and E the acceleration voltage of the microscope in Volts
in MAUD H can be:
a refineable thickness parameter
the anisotropic crystallite size used for line broadening
H

## Slide 18
Structural Analysis of Nanomaterials
using Electron Diffraction
pattern matching
structure factors
kinematical approx.
Blackman correction
(2-beams interactions)



► Electron crystallography: more complicated than XRD due to dynamical conditions

## Slide 19
pattern matching
structure refinement
a=4.5853(3)Å c=2.9448(3)Å
x(O1)=y(O1)=0.3006(2)
Blackman 2-beams correction
x(O1)=y(O1)=0.3064(2)
a=4.5875(2)Å c=2.9475(2)Å
Structural Analysis of Nanomaterials
using Electron Diffraction
XRPD
a=4.584(1)Å c=2.949(1)Å
x(O1)=y(O1)=0.3062(5)
POPA
R0 + R1
2-beams
more reliable results
for structure refinement